CHARLES DOUGLAS GILDING STUDIO

3815 4th Ave NE

Seattle, WA 98105

Phone: 206.795.8376

charles.studio@usa.net

gildingstudio.com

~

Crackle Gesso

Gothic, Deep Cracks

RATIO 1:1:1 (Total RSG and Hide Glue: Whiting: Corn Starch (100 is 1 part)

50 Grams 10% Rabbit Skin Glue Solution (5g dry RSG: 45 ML Distilled Water)
50 Grams 50% Hide Glue Solution (25g dry Hide Glue : 25 ML Distilled Water)

100 ML Distilled Water

100 Grams Calcium Carbonate (also known as ‘whiting’ or ‘chalk’)
100 Grams Corn Starch

Medium Crackle

RATIO 2:2:1 (Total RSG and Hide Glue: Whiting: Corn Starch – (50 is 1 part)

50 Grams 10% Rabbit Skin Glue Solution (5g dry RSG: 45 ML Distilled Water) 
50 Grams 50% Hide Glue Solution (25g dry Hide Glue: 25 ML Distilled Water)

100 ML Distilled Water

100 Grams Calcium Carbonate (also known as ‘whiting’ or ‘chalk’)
50 Grams Corn Starch

Heat, mix, and strain
Apply minimum 6 coats (more for deeper crackle)
Either dry naturally for gentler crackle or use a hair dryer for deeper crackle
Spray with water/alcohol before using hair dryer to help create deep crackling (repeat process several times)

Materials

HG31503/1 – Hide Glue, (1 Pound; 240 Bloom Strength recommended for moderate crackle. Higher bloom strength 315 High Stress for deeper crackle) …(240 Bloom Available at Gilded Planet)

RSG330/1 – Rabbit Skin Glue (1 Pound) …(350 Bloom Available at Gilded Planet)

Carb3/1 – Calcium Carbonate (1 Pound) …(Available at Gilded Planet)

Corn Starch…(Buy Local)

Water, Distilled if available (Buy Local)