CHARLES DOUGLAS GILDING STUDIO

3815 4th Avenue NE

Seattle, WA 98105

Phone: 206.795.8376

charles.studio@usa.net

www.gildingstudio.com

Gold Leaf Gilding

GILDER'S TOOLS & MATERIALS

Recommended styles and sizes

TRADITIONAL WATER GILDING

I.  Tools

a. Gilder's Pad (To lay gold for cutting)

7 x 9 ½”" with parchment wind shield or without

Italian: GP/D Deluxe	(Included in Gilded Planet Kit)

b. Gilder's Knife (To cut gold)

5 1/2" single edge blade, flat tip

German: GK/S (Included in Gilded Planet Kit)

c. Gilder's Tip (To pick up gold)

Single thick, squirrel hair, 3 3/4" - 4"

French: 213S/3, Squirrel Hair (Included in Gilded Planet Kit)

d. Agate Burnisher (Dog’s Tooth shape). Approx.¾” Stone

German: SL-6 (Included in Gilded Planet Kit)

e. Gilder's Mop

Pure Squirrel hair, pointed edge (collect small to large mops)

61/2: Pure Kazan Squirel, pointed (Included in Gilded Planet Kit)

f. Gesso Brush

Black, Dark Ox hair, 3/4" or 1”

German: #D660/3/4 ,beveled Edge, (Included in Gilded Planet Kit)

French: 223/16 (1” Stipple) (Optional for the future; Available at Gilded Planet)

g. Wash Brush for patinating; 625/1 Habico, Tapered/Mixed Squirrel Hair
    (Included in Gilded Planet Kit)

h. Stencil Brush, used as a Bole Burnishing Brush 
   432/10 (Optional for the future, available at Gilded Planet)

CHARLES DOUGLAS GILDING STUDIO

3815 4th Avenue NE

Seattle, WA 98105

Phone: 206.795.8376

charles.studio@usa.net

www.gildingstudio.com

www.gildingstudio.blogspot.com

Gold Leaf Gilding

GILDER'S TOOLS & MATERIALS

Recommended styles and sizes

II. Materials

a. Calcium Carbonate (For gesso)

French, Italian, or American; 1 lb.

Carb3/1: Florence Rouge from Vermont (Included in Gilded Planet Kit)

b. Rabbit Skin Glue

Pebble or Granular (German)

Framer’s Glue: 309/1 (granulated) (Included in Gilded Planet Kit)

c. Clay Bole

Pre-mixed, Selhamin (German), Red, Yellow

3355P/K: Selhamin Red pre-mixed, one Kilogram

(Small amount - 5 oz -  Included in Gilded Planet Kit for class project)

d. Gold Leaf (Recommended Brand Manetti as one high quality choice).

25 leaves per book, 20 books per pack

MA23.0DB: 23k Double Gold Leaf Booklet (Included in Gilded Planet Kit)

e. Rottenstone (light abrasive and toning powder)
  	    (Available locally or available through Gilded Planet)

f. Knead-a-Mold

CHARLES DOUGLAS GILDING STUDIO

3815 4th Avenue NE

Seattle, WA 98105

Phone: 206.795.8376

charles.studio@usa.net

www.gildingstudio.com

www.gildingstudio.blogspot.com

Gold Leaf Gilding

GILDER'S TOOLS & MATERIALS

Recommended styles and sizes

TRADITIONAL WATER GILDING

General Studio Tools for Preparing Materials for Traditional Water Gilding

l. Plastic Cups (For storing prepared gesso and clay; may be used during     application)

Kitchen-Use style with lids

2 small, 2 medium sized

2. Selection of Glass Jars for storing prepared gesso and clay bole, variety of sizes.

3. Cotton: Pharmaceutical preferred, roll or cotton balls (not polyester)

4. Isopropyl Alcohol (70%, verify no acetone ingredient)

5. Sandpaper: Wet & Dry, 1,000 & 600 grit; also 3M if possible, 120, 220, 280, 320 grit

6. Gesso Re-Cutting Tools (optional; for advanced techniques)

Contour Sanders (concave and convex)

7. Double boiler (cooking pot inside a cooking pot) (Buy Local)

8. ‘Little Dipper’ Crock Pot to keep gesso and bole warm (Buy Local or     Amazon)

9. Fifth Burner for heating pot of water.

10. Waterstone: For removing nicks in knife; (Online at: ‘Rockler’,  800/4000 Grit). or 1000 Grit sandpaper as an option.)

CHARLES DOUGLAS GILDING STUDIO

3815 4th Avenue NE

Seattle, WA 98105

Phone: 206.795.8376

charles.studio@usa.net

www.gildingstudio.com

www.gildingstudio.blogspot.com

Gold Leaf Gilding

GILDER'S TOOLS & MATERIALS

Recommended styles and sizes
(Continued)

11. Distilled Water

12. Argan Hair Oil or Badger Hand Balm (Natural; use on arm with Gilder's Tip to pick up gold leaf).  https://www.badgerbalm.com/c-28-body-hand-moisturizers.aspx

13. Metric Scale (For measuring materials)

14. Sifter (For sifting whiting); Plus Mixing Small, Medium Spoons, Spatula

15. Mixing Bowls, Stainless Steel. 2 Medium Size, 2 Large (for making Gesso and Clay Bole)

CHARLES DOUGLAS GILDING STUDIO

3815 4th Avenue NE

Seattle, WA 98105

Phone: 206.795.8376

charles.studio@usa.net

www.gildingstudio.com

www.gildingstudio.blogspot.com

Gold Leaf Gilding

GILDER'S TOOLS & MATERIALS

TRADITIONAL WATER GILDING

Toning Materials (Partial listing of available materials)

1.  Casein (Rosco Iddings preferred brand)

 Raw Umber, Burnt Umber, Burnt Sienna, Raw Sienna

2.  Dry Pigment

 Raw Umber, Raw Sienna, Ultramarine Blue, Yellow Ochre, White, Black

3.  Pumice Powder

4.  Rottenstone

5.  Oil Free Steel Wool

 "0000" grade

6. Cotton

 Pharmaceutical preferred, sterile roll or cotton balls

7. Shellac

 Blonde Dewaxed Shellac Flakes

 Ruby or Orange Shellac Flakes

8. Calcium Carbonate (for making rubbing paste).

9. Denatured or Ethyl Alcohol (for making rubbing paste)

10. Distilled Water

12. Polyvinyl Acetate (PVA Glue); White Glue (Elmer’s Glue)

CHARLES DOUGLAS GILDING STUDIO

3815 4th Avenue NE

Seattle, WA 98105

Phone: 206.795.8376

charles.studio@usa.net

www.gildingstudio.com

www.gildingstudio.blogspot.com

www.instagram.com/gildingstudio

Gilding Glossary

Burnish: The process of polishing gold leaf with a stone, usually an agate, to bring the leaf to a brilliant luster. Only water gilded leaf where gesso and bole is used may be burnished with a stone.

Backing Up: A term used in painting the back of gold or silver leaf on the reverse of gilded glass.

Clay Bole: A special earth clay, available in a variety of colors, applied over gesso. Provides an attractive hue under gold leaf and acts as a cushion against the hardness of gesso during burnishing.

Distress: Partial removal of gold or metal leaf to show the underlying clay bole or tinted oil size ground. Simulates a worn appearance.

Dragon’s Blood / Gamboge: Resins used to tint shellac and lacquers which are applied over silver or aluminum leaf to obtain a golden glow. Their use goes back to medieval times.

Etching: The term used in scratching through gold or silver leaf on gilded glass to help create an image siewed from the front of the glass.

Gesso: Mixture of glue and whiting (precipitated chalk) applied over wood to fill the grain and provide a smooth, hard surface to gild upon. Allows gold leaf to be burnished in traditional water gilding.

Gilding: The application of a very thin gold or metal leaf over another object, often frames, furniture, and architectural detail.

Gold Beating: The process of beating gold into thin leaves, usually measuring 3-3/8” square. Available in numerous shades and karats ranging from 12K white gold to 24K gold. Seattle Gold Leaf offers gold leaf from France, Germany, Japan, Australia, and Italy.

Modern Gold: Specifies a gilded finish that appears solid, brilliant, and new. A rubbed, distressed finish may be applied to show underlying color ground.

Old Gold: The appearance of age and wear in the gilded finish achieved through various treatments.

Patination: The process of applying a patina to the gilded surface. Includes the use of pigments and distressing to simulate age and wear.

Toning: The treatment of the gilded finish including burnishing and/or patination to achieve a desired effect.

CHARLES DOUGLAS GILDING STUDIO

3815 4th Avenue NE

Seattle, WA 98105

Phone: 206.795.8376

charles.studio@usa.net

www.gildingstudio.com

www.gildingstudio.blogspot.com

www.instagram.com/gildingstudio

Gilding Glossary
(Continued)

Shell Gold: Gold leaf that is ground with honey with a mortar and slab, filtered, and mixed with gum arabic. Used as a water-soluble agent for touch-ups. Formerly made in a ‘shell’ during the medieval period.
Size: The binder used in gilding to adhere or assist in attaching gold, silver or other leafs in gilding to a prepared surface. This may include oil size (a varnish used in oil gilding), gelatin and water for glass gilding/verre eglomise, gum ammoniac in water, water and alcohol (for traditional water gilding).

CHARLES DOUGLAS GILDING STUDIO

3815 4th Avenue NE

Seattle, WA 98105

Phone: 206.795.8376

charles.studio@usa.net

www.gildingstudio.com

www.gildingstudio.blogspot.com

www.instagram.com/gildingstudio

Gold Leaf Gilding

LITERATURE

Gilded Wood, Conservation and History

36 essays by a team of leading International experts; illustrated; 432 pages

Sound View Press

170 Boston Post Rd.  Madison, CT 06443

Telephone:  203-245-2246

Gold Leaf, Paint & Glass

Frances Federer

Contemporary Book on the ancient artform of Verre Eglomise

Thomas Publications; London

The Craftsman's Handbook (Il Libro dell'Arte)

Cennino d'Andrea Cennini

Translated by Daniel V. Thompson, Jr.

The Practice of Tempera Painting

Materials and Methods

Daniel V. Thompson, Jr.

Practical Gilding

Peter & Ann MacTaggart

Excellent handbook concerning gilding methods.

Published by Mac & Me LTD., Welwyn, Herts, England AL69EU

The Gilder's Manual

(Reprinted by Society of Gilders)

19th Century formulas, originally published in 1876.  Available from:  SOG Products,

P. O. Box 50179, Washington, D.C. 20091

CHARLES DOUGLAS GILDING STUDIO

3815 4th Avenue NE

Seattle, WA 98105

Phone: 206.795.8376

charles.studio@usa.net

www.gildingstudio.com

www.gildingstudio.blogspot.com

www.instagram.com/gildingstudio

Gold Leaf Gilding

LITERATURE
(Continued)

Gold Leaf Techniques

Raymond J. Leblanc; Revised by O. Sarti

Excellent book on oil gilding and glass gilding.

The Signs of the Times Publishing Company,

Cincinnati, Ohio

The Frame in America, 1700-1900

William Adair

A survey of fabrication techniques and styles.

Professional Picture Framers Association Educational Foundation, Inc.

CHARLES DOUGLAS GILDING STUDIO

3815 4th Avenue NE

Seattle, WA 98105

Phone: 206.795.8376

charles.studio@usa.net

www.gildingstudio.com

www.gildingstudio.blogspot.com

www.instagram.com/gildingstudio

Gold Leaf Gilding

ORGANIZATIONS (US)

The American Institute for Conservation of Historic and Artistic Works (AIC)

1400 Sixteenth Street NW, Suite 340

Washington, DC 20036

Telephone: 202-232-6632; FAX: 202-232-6630

Western Association for Art Conservation (WAAC)

12135 Mitchell Avenue #101

Los Angeles, CA 90066

The Society of Gilders

Email: information@societyofgilders.org

www.societyofgilders.org

SUPPLIERS

www.GildedPlanet.com (Online Retailer for Gold and Silver Leaf and Supplies; Ships Internationally, No Minimum Required))

Sepp Leaf Products (Wholesale Account Required)

381 Park Ave. S #1301

NY, NY 10016

Telephone: (212) 683-2840

Rosco/Iddings Deep Colors Casein

http://us.rosco.com/en/product/iddings-deep-colors

Seattle: PNTA, 2414 SW Andover Street

The Decorator’s Supply Corporation

Composition Ornaments (Compo)

3610-12 S. Morgan Street

Chicago, Il 60609

Telephone: 773-847-6300

CHARLES DOUGLAS GILDING STUDIO

3815 4th Avenue NE

Seattle, WA 98105

Phone: 206.795.8376

charles.studio@usa.net

www.gildingstudio.com

www.gildingstudio.blogspot.com

www.instagram.com/gildingstudio

Gold Leaf Gilding

SUPPLIERS (Continued)

Daniel Smith Fine Artist's Materials

4150 First Avenue South

P. O. Box 84268

Seattle, WA  98124-5568

Telephone: 206-223-9599; FAX: 206-223-0672

www.danielsmith.com